## Slide 1
Excursion #2
We shall meet the chiral anomalies as they appear already in simplest, MF or BCS types, models particularly at finite temperatures when normal excitations are present.
The resulting effective Ginzburg-Landau theory will prove to be quite different from what is commonly expected.
After collaboration with Natasha Kirova in 1999 and 2018-9
Inspired by experimental studies in Grenoble by P. Monceau et al
and at Cornell, R. Thorne group

## Slide 2
John Bardeen’s Grand Unification:
……
1940’s - transistor
1950’s - Superconductivity
1976 – 30/01/1991- - Charge Density Waves
Common features of incommensurate CDWs and the superconductors:
Ocdw =Acos(2KFx+ φ)  complex order parameters Ocdw,sc ~ A exp[i]
hence vortices  dislocations, phase slips  phase solitons
Similar microscopic theories: Peierls-Frohlich vs BSC
Pair-breaking gaps 2D - hence tunneling, FFLO  solitonic lattices
Tighter links at D=1: Spinons as amplitude solitons
Phases cdw , sc are in conjugation: [i, ∂xj]~d(x)
2D becomes the common spin gap; broken pair becomes 2 free spinons
The same current is j=- ∂tcdw /π ∂xsc the local density =- ∂xcdw /π CDW wave number shift Q=∂xcdw

## Slide 3
Collective motion of electronic crystals:
Incommensurate CDWs, SDWs, Wigner crystals:
Frohlich conduction by the collective sliding.
Topological defects: solitons, dislocations (electronic vortices).
Current conversion among normal and condensed electrons.
Phase slips in nano-junctions.
While the phase velocity or deformation is the principle ingredient,
no collective effects can set in without deformations of the CDW amplitude A(x,t),
particularly with A passing though zero.

## Slide 4: Dynamic origin of dislocations
CDW sliding in the applied external electric field – collective motion of electronic crystal .
To set it in motion at different velocities:
Transfers flow of vortices – thick channel
Coherent phase slip - thin cannel
(Maki & Ong, Gorkov)
source
drain
v=0
vI
Formation of new planes in the electronic crystal
Elimination of additional planes
Direct access to the current conversion via dislocations: Space resolved X-ray studies
Phase slips:
Microscopically – selftrapping of electrons into solitons, their subsequent aggregation
Macroscopically – the edge dislocation line proliferating/expanding across the sample.
enhanced v
ceased curent
normal v
the material flow; its conversion provides the climb of dislocations.
proliferation of a dislocation line.
Static origin of vortices in analogy to SCs

## Slide 5
Solid lines: maxima of the charge density. Dashed lines: chains of the host crystal.
Topological defects in a CDW.
Embracing only one chain of atoms, the pairs become a vacancy or an interstitial  ± 2p solitons in CDW
By passing each of these defects, the phase changes by 2p. Far from the defect the lattice is not perturbed.
At the (red) front line the defected chain is displaced by half of period.
Along the defected chain the whole period ±2 is missed or gained

## Slide 6
Ginzburg-Landau – like model
Only extrinsic (other bands) carriers n are taken explicitly.
In the GL spirit, the intrinsic carriers (in the gap region) are integrated out, their effect is hidden in the CDW amplitude A.

## Slide 7
Many vortices appear temporarily in the course of the evolution.
For that run, only one will be left.
nucleations
traces of A=0
Numerical modeling of nonstationary processes in CDWs within the TDGL phenomenology T. Yi, A. Rojo, N. Kirova and SB.
The result is as spectacular as it is wrong!
The TDGL approach is principally deficient here.

## Slide 8
Well established and works for stationary state and as a tool to reach it. Takes explicitly the extrinsic carriers (not interacting with the CDW)
Restrictions:
The intrinsic carriers have been integrated out and come into the model only via the order parameter amplitude A.
Major problem:
Violation of the local charge conservation for the condensate .
In our case A(x,y,t)0
automatically if A = const
Deadly problems with the TDGL model for CDW
Way of resolution: keep carriers in hand and decompose A2

## Slide 9
More general scheme :
1D intrinsic carriers are taken explicitly into account
Forbidden : scattering in the frame of the host lattice - no impurities
Allowed: scattering by CDW phonons; electronic collisions
=(+,- ), order parameter ei

## Slide 10
Chiral transformation:
Interactions depends only on derivatives of , i.e: no Umklapp processes , Electrons scatter on each other and on CDW phonons

## Slide 11
can choose
False local “gauge” invariance – the potential can be excluded at no cost
PROBLEM 1
In absence of normal carriers we definitely expect:
- Not a full square of the chiral-invariant combination:
2 looks to be an anomaly - and not only
Action = free energy W after integration over fermions:

## Slide 12
For conducting electrons
By definition :
T
We
Tc
T
We
Tc
We obtain:
We expected to have:
PROBLEM 2

## Slide 13
Resolution: the whole expression has been lost
Chiral anomaly
Now, for linearized eqs. and with constant ρn=1-ρc
The contribution of normal carriers bites from the T=0 anomalous action erasing it down to zero at Tc when A0, ρcA2
In relativistic field theory language (I. Krive and A. Rozhavsii for CDWs at T=0):
-eE

## Slide 14
nin, nex concentrations of intrinsic and extrinsic free carriers
F(A,nin,nex) static free energy, not additive any more
Its minimum at A≠0 is erased at nex above a critical value (vortec core)
Nonlinear regime. Local energy functional
Expect A2 - actually 1. Non analytic in Ψ Both terms are not derivable perturbatively – the chiral anomaly.
+ need a mechanism for nin to compensate ∂ at A→0

## Slide 15
Possible simplifications and explitness Infinite conductivity: - a bridge to the naive GL eqs.
LHS resembles the static effective charge nc=A2∂x/ - identifying ρc and A2 But instead: ∂xnc= ρc ∂x2 /
Never a closed expression for j
screening of Ex with a standard local screening length l2=r02/ ρn
Poisson eq.
Phase eq.
Resembles GL with ρc as A2 but with no differentiation of the amplitude :
ρc∂x instead of ∂x(A2) ρc ∂x2 instead of ∂x(A2∂x )
Not like variational eqs.

## Slide 16
Nonanalytic dependence on the amplitude requires new more complicated numerical studies.
We still can run up to nucleation of vortices at a surface.
But then the program crashes and we cannot trace proliferation of vortices as before.
A price for no explicit compensation of diverging ∂ by vanishing A2

## Slide 17
Thanks to substantial simplifications of the free energy form:

## Slide 18
Chiral transformations with account for chiral anomaly were applied to the CDW model
Two-fluid hydrodynamics was constructed for the order parameter and the normal liquid
Topologically nontrivial dynamics appears under applied fields or charge injection
Spontaneous space-time vorticity under the driving current was modeled numerically some under simplifications, periodic sequence of amplitude nodes with 2π phase increments was demonstrated
The numeric procedure needs to be stabilized for the nonanalytic eqs.
The problems of glide and climb should be considered
Conclusion and perspective.